## Slide 1: Service Life Estimate for the ALCM Fuel Boost Pump Electronic Unit (FBPEU)
FOUO
Unclassified
Viet Tran
AFNWC/NDMEA
29 Sep 2016

## Slide 2: Overview
BLUF
Problem
Function & Location of FBPEU
Data Sources
  ACI, REMIS Level 1 Pass Rate, Level 1 Regression Analysis
  ASIA
    Function Test Output Analysis, Teardown, Piece part Performance
Selecting Failure Mechanism (FM)
Analyze and Research Selected FM
Determine Scale Parameters & Reliability Function
Summary
Recommendations
FOUO
Unclassified
FOUO

## Slide 3: BLUF
Fuel Boost Pump Electronic Unit (FBPEU) has an estimated service life of 2060
EMI protection assurance risk is at 2023
FOUO
FOUO

## Slide 4: The Problem
Certain ALCM components are showing higher failure rates. These items are expected to impact the fleet over time.
MSD conducted a Service Life Estimate on the Fuel Boost Pump Electronic Unit (FBPEU) to support future missile sustainment decisions.
FOUO
FOUO

## Slide 5: FBPEU Function and Location
Function - FBPEU converts 28 Vdc power to 28 Vac power for use by the fuel pump
Location - FBPEU is mounted in the aft (engine) compartment of the missile
FBPEU Location
Note: An AC motor eliminates reliability problems associated with DC brushes
FOUO
FOUO

## Slide 6: Analytical Condition Inspection (ACI)
ACI Visual Inspection
  No record of discrepancy
ACI Functional Test
  100% pass rate since 1992 – 2015
FOUO
FOUO

## Slide 7: Level 1 Pass Rate Analysis
REMIS Level 1 Pass Rate
  No failures in the past 5 years
Year | 2010 | 2011 | 2012 | 2013 | 2014 | 2015
Total of FBPEU Failure | 0 | 0 | 0 | 0 | 0 | 0
Total Number of Level 1 Test | 85 | 250 | 314 | 257 | 288 | 224
Level 1 Pass Rate | 100% | 100% | 100% | 100% | 100% | 100%
Allocated Reliability Spec (Threshold) | 99.8% |  |  |  |  | 

## Slide 8: Regression Analysis – Throttle Command
FBPEU Level 1 Results 2001 - 2014
Linear Regression indicates no significant trend
Normal Distribution shows consistency within performance margins

## Slide 9
FBPEU Level 1 Results 2001 - 2014 Cont.
Linear Regression indicates no significant trend
Normal Distribution shows consistency within performance margins
  Regression Analysis –
  Fuel Control Actuator Position

## Slide 10: Functional Test Results
  Functional test on 10 FBPEUs from supply (2016)
    9 passed all parameters
    1 failure – possibly due to test set up.
      E-spectrum “One theory concludes that the manual test procedure used by the depot is prone to test setup errors and could easily lead to this type of failed indications”
FOUO
FOUO

## Slide 11: Function Test Output Analysis
1 out of 25 parameters showed a trend
Slope of -.4 Hz per year, age of the FBPEUs tested was estimated based on serial number
FOUO
FOUO

## Slide 12: Teardown Analysis
3 FBPEUs were sent to E-spectrum for teardown analysis
Visual Inspection – Microcircuits show no irregularities or anomalies
60 piece parts selected for electrical parameter performance analysis (summary on next slide)
  In-Depth Laboratory Analysis (Scanning Electron Microscope (SEM) & Energy Dispersive X-ray Spectroscopy (EDS)) 2 samples of each below:
    Operational Amplifier, NPN Transistor, PNP Transistor, Transistor (OEM Unique), High Power Silicon Transistor, Microcircuit Voltage Comparator and Zener Diode show no evidence of any type of damage or aging
    Wet Tantalum Capacitors showed electrolyte leakage

## Slide 13: Component Level Electrical Parameter Performance
  Electrical Parameter Performance Test results from 60 piece parts
  2 components exhibited test failures
    A1C2 Wet Tantalum Capacitor from FBPEU S/N 398
      Evidence supports manufacturing defect (low volume of electrolyte)
      (Note: FBPEU S/N 398 passed all test parameters during functional testing)
    A3R1 Metal Film Resistor from FBPEU S/N 1095
      Specification allows 1% tolerance; test shows 4 % drift value
    (Note: FBPEU S/N 1095 passed all test parameters during functional testing)
FOUO
FOUO

## Slide 14: Selected Failure Mechanism
    WTC
      Open circuit due to electrolyte leakage (well known issue in industry)
    Metal Film Resistor
      Resistance drifts higher with age due to thermal and electrical stress (well known issue in industry)
FOUO
FOUO

## Slide 15: WTC Failure Mechanism
WTC Failure Mechanism
  Electrolyte (Sulfuric Acid H2SO4) leakage over time due to glass seal rupture, causes loss of capacitance which creates an open circuit
Vishay Intertechnology INC.
FOUO
FOUO

## Slide 16: WTC Location
A1 Circuit card (EMI filter) contains 5 WTCs
  WTCs below are in parallel
FOUO
FOUO

## Slide 17: WTC X-Ray
2 samples obtained from FBPEU S/N 398 Energy Dispersive X-Ray Spectroscopy (EDS)
  Sample A (C2) was comparatively dry (i.e. little or no visible liquid after dissection), EDS shows no Sulfuric Acid on the glass seal surface, the cause of low levels of electrolyte could be not enough volume added during fabrication
  Sample B (C3) electrolyte leaked past the swaged anode lead, EDS shows Sulfuric Acid has reached the glass seal surface. However, it passed Electrical Parameter Performance Test
Sample A
Sample B
Sulfuric Acid
FOUO
FOUO
Notes: Note: The disassembly activities required to remove the capacitor (Sample A) from the A1 Electronic Assembly resulted in some grinding on the metal case of the capacitors and most certainly resulted in this deposit of metal fines ( hot particle) in the glass seal.

## Slide 18: WTC Electrolyte Research
FAILURE MECHANISMS IN WET TANTALUM CAPACITORS ( Plessey Company Limited June 17, 1975)
  The electrolyte boils at 128C (262F) at atmospheric pressure and hence considerable pressure develops at high temperature. However, there is a considerable safety margin for tubular units, normally rated up to 125C (257F), before actual seal rupture will occur.
  At low temperature, the electrolyte used in devices rated to -55C freezes at -64C giving an open circuit. However, as soon as the temperature is raised the electrolyte melts and works normally. Thus, indefinite storage at-60C is quite permissible.
FOUO
FOUO

## Slide 19: WTC Electrolyte Research
FAILURE MECHANISMS IN WET TANTALUM CAPACITORS (Plessey Company Limited June 17, 1975)
“The wear-out mechanism of wet tantalum units is the loss of water vapor leading to open-circuit, although at rated temperatures, long life times are achieved”
FOUO
FOUO

## Slide 20: Stress Cycles Assumption
Assumption:
ASIA teardown shows evidence of the onset of Electrolyte leakage which can take many years to complete. The WTC under evaluation are not exposed to high electrical stress condition but are exposed to many years of ambient thermal cycling which has a smaller effect on integrity of the seal. This calculation assumes the total failure mechanism full maturity is approximately 100 years (Eta median = 50 years)
Research shows WTC slope parameter (Betas) can range from 1.5 to 5. This calculation assumes a Beta of 3 due to the lack of test data
Based on data analysis and X-Ray results (initial stages of electrolyte leakage), the observed failure free life (Upsilon) of the WTC is estimated to be 25 years
Operational Margin (years) cannot be determine at this time due to the placement of the 5 parallel WTCs on the A1 circuit card in a configuration design for EMI protection (not detectable for normal ops)
FOUO
FOUO

## Slide 21: Reliability Function Based On Weibull Distribution
  Eta equal to 50 years (failure mechanism maturity )
    scale parameter - scales the curve along the x axis - time, cycles, etc.
  Beta equal to 3 (rate of failure mechanism maturity)
    shape parameter - or slope
  Upsilon equal to 20 years (failure free life)
    location parameter
  Operation Margin – 0 years

## Slide 22: LRU Hardness Assurance
Chart: 
Projected hardness assurance of the FBPEU
Hardness Assurance Threshold 98%
Today
FOUO
FOUO

## Slide 23: Hardness Assurance Risk
(EMI Filter) Hardness Assurance Risk based on the 2% degradation by 2023
  WTC degradation will continue to accelerate
Note: Recent ALCM High Electro-Magnetic Pulse (HEMP) testing (2015 - 2016) verified hardness shielding integrity
Notes: HEMP testing consist of two part: Skin-on and Cable shielding (Skin off).
Skin-on showed ALCM had proper shielding against HEMP
Skin-off showed cable shielding had proper EMP hardness protection during HEMP

## Slide 24: Metal Film Resistor (MFR) Failure Mechanism
MFR Failure Mechanism
  Thermal cycling effects film stability leading to oxidation of the resistance alloy and changing electrical characteristics
Ceramic Carrier
Thin Metal Film
End Cap with leads
FOUO
FOUO

## Slide 25: MFR Location
A3 Circuit Card - Oscillator Control
(E-spectrum ASIA) Metal film resistor which has a robust structure that reduces sensitivity to most factors leading to instability and eventual change or drift in its’ resistance value. Since this particular resistor is in the oscillator circuit, and is connected to an external connector pin, the possibility of repetitive stress, as well as stress from an external component failure is in play
FOUO
FOUO
Notes: Thermal cycling effects film stability leads to oxidation of the resistance alloy, this could cause change in electrical characteristics

## Slide 26: Metal Film Resistor (MFR) Stability
The stability of a resistor depends primarily on its history of exposures to temperature changes. Stability is mainly affected by:
  1) Changes in the ambient temperature and heat from adjacent components
  2) Destabilizing thermal shock, caused by a sudden application of power
  3) Long-term exposure to high temperature and applied power (load-life stability)
  4) Repetitive stresses from being switched on and Off
Above conditions are not anticipated for FBPEU’s components
This resistor experiences normal environmental thermal cycles which will slightly accelerate resistance drift due to age
FOUO
FOUO

## Slide 27: MFR Service Life Factors
MFR characteristics
  MFR design = 22.8k +/- 1% ohms
  Electrical performance test shows resistance drift of 2.77%
Assumptions
  Near linear drift (commonly known)
  Circuit card assembly tolerance 3%
  LRU operational design tolerance 5%
  Resistance drift impacts LRU operation at 7% (Operational Design + 2%)
  No extreme thermal or electrical stress
FOUO
FOUO

## Slide 28: MFR Resistance Drift Maturity
Chart: 
Projected service life estimate of the FBPEU is 2060
FOUO
FOUO

## Slide 29: Summary
FBPEU ACI 100% pass rate, Level 1 100% pass rate, functional test indicated only 1 parameter with trend and teardown analysis identified limited age related effects
MFR resistance drift will likely impact Oscillator (A1circuit card) frequency and voltage over time. However, the drift detected in functional testing is many years from reaching the estimated operational margin
WTC electrolyte leakage will likely create an open circuit in the EMI filter (A3 circuit card). However, this risk applies to electromagnetic hardness protection, not to functional operation
Both MFR and WTC performance will be simulated in PSPICE to determine critical operational margins

## Slide 30: Recommendation
Recommended Next Steps
  Rate FBPEU Green on ALCM Technical Assessment
  Simulate FBPEU performance in PSPICE
  Continue to monitor through ACI functional testing

## Slide 32: Back Up
Test Out Put Sample

## Slide 34: WTC Comparison
Comparing WTC
WTC on WAD CB3. Silver migrating (metal migration) across the glass seal toward the lead. (Note: These capacitors are used in the impact sensor trigger circuit to provide the final fuzing signal to the warhead)
WTC on FBPEU A1 Card. Due to similar design, it is likely the same failure mechanism exist. However, Silver migrating showed no signs of this condition in the two samples analyzed
WAD CB3
WAD WTC

## Slide 35: Vishay Spec
Mil-PRF-55182 (Vishay Intertechnology INC.)
  Failure Rate % per 1000 hours = 0.001%
  Power ratings are based on the following two conditions:
    ± 2.0% maximum ΔR in 10000 hours load life.
    + 175°C maximum operating temperature

## Slide 36: MFR Comparison
Recent ASIA shows Elevon Actuator Controller is also contains RNC55 Metal Film Resistor
  Two samples from EAC ASIA were tested for electrical performance, both measured outside of threshold limitation. However, other inspection such as X-ray, SEM, and disassemble visual inspection shows no anomalies

## Slide 37: OPERATIONAL THRESHOLD
  MSD creating an electronic circuit simulation of FBPEU circuit card assemblies to determine better estimate of operational margin
  FDE & FGT confirmed no failure due to FBPEU degradation
  Operational threshold is set at operational design plus an additional 2% of resistance drift